## Slide 1
RECIPROCAL LATTICE & X-RAY DIFFRACTION
B.Sc. II Physics • Crystal Structure
Dr. Sandip S. Patil Department of Physics

## Slide 2
Learning Outcomes
Define reciprocal lattice and explain its construction from a direct lattice.
State important properties of reciprocal lattice vectors and planes.
Explain X-ray diffraction using Bragg’s law and the Ewald construction.
Distinguish Laue, rotating-crystal and powder photograph methods.
Analyse a cubic crystal from powder diffraction lines using d-spacing and indexing.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 2

## Slide 3
Why Do We Need Reciprocal Lattice?
Direct lattice
Describes periodic positions of atoms in real space.
Useful for crystal geometry and unit cells.
Diffraction
X-rays are waves. Diffraction depends on directions and spacings of crystal planes.
Reciprocal lattice
Transforms plane geometry into point geometry in k-space.
Diffraction conditions become simple vector relations.
Real space ↔ Reciprocal space
Each set of crystal planes (hkl) corresponds to one reciprocal-lattice point G_hkl.
The vector G_hkl is normal to the (hkl) planes.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 3

## Slide 4
Reciprocal Lattice: Definition
To a direct lattice with primitive vectors a, b and c, associate reciprocal primitive vectors a*, b* and c*.
The reciprocal vectors are defined so that a*·a = b*·b = c*·c = 1 and cross terms are zero.
Depending on convention, a 2π factor is included. Here the crystallographic convention is used.
a* = (b × c) / [a · (b × c)]
b* = (c × a) / [a · (b × c)]
c* = (a × b) / [a · (b × c)]
With 2π convention
a* = 2π(b×c)/[a·(b×c)]
Then |G_hkl| = 2π/d_hkl.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 4

## Slide 5
Construction of a 2-D Reciprocal Lattice
a
b
Direct lattice
a*
b*
Reciprocal lattice
Reciprocal lattice points are indexed by (hkl).
The spacing between reciprocal points is inversely related to real-space plane spacing.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 5

## Slide 6
Important Properties of the Reciprocal Lattice
1. Plane normal
G_hkl is perpendicular to the family of (hkl) planes.
2. Magnitude
|G_hkl| = 1/d_hkl (crystallographic convention).
3. Indexing
The reciprocal point is labeled (hkl), matching the plane indices.
4. Diffraction
Diffraction occurs when the scattering vector equals a reciprocal-lattice vector.
5. Reciprocal of reciprocal
The reciprocal lattice of the reciprocal lattice reproduces the direct lattice (with the chosen convention).
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 6

## Slide 7
Reciprocal Lattice of Cubic Crystals
Simple Cubic (SC)
Direct: SC
Reciprocal: SC
Lattice constant: a* = 1/a
Body-Centred Cubic (BCC)
Direct: BCC
Reciprocal: FCC
Lattice constant: a* = 2/a (with equivalent conventional-cell scaling)
Face-Centred Cubic (FCC)
Direct: FCC
Reciprocal: BCC
Reciprocal and direct structures interchange.
For cubic crystals: d_hkl = a / √(h² + k² + l²)
Thus reciprocal-space distance from the origin is directly linked to 1/d_hkl.
This relation is central to powder diffraction indexing.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 7

## Slide 8
Diffraction of X-Rays by Crystals
X-rays have wavelengths (~0.1 nm) comparable to interatomic spacings in crystals.
Atoms scatter the incident X-ray wave. The periodic crystal arrangement causes interference.
Constructive interference produces intense diffraction maxima.
Diffraction maxima reveal lattice spacings, symmetry, crystal structure and phase information.
Incident waves
Crystal planes / atoms
Path difference = 2d sinθ
Constructive: 2d sinθ = nλ
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 8

## Slide 9
Bragg’s Law
Crystal planes
θ
θ
2d sinθ = nλ
Meaning
d = interplanar spacing
θ = Bragg angle
λ = X-ray wavelength
n = order (1, 2, 3, …)
For first-order diffraction, n = 1 is most commonly used in powder analysis.
The measured peak position 2θ gives d once λ is known.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 9

## Slide 10
Bragg’s Law in Reciprocal Lattice
In reciprocal space, diffraction is expressed through the scattering vector Δk.
The incident and diffracted wavevectors have equal magnitude: |k| = 1/λ (crystallographic convention).
Diffraction occurs when Δk reaches a reciprocal-lattice point G_hkl.
O
kᵢ
k_f
G = k_f − k_i
|G_hkl| = 1/d_hkl = 2 sinθ / λ
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 10

## Slide 11
Ewald Construction
Draw the incident wavevector k_i from the origin O.
Construct a sphere of radius |k| = 1/λ (or 2π/λ with the 2π convention) centered at the tip of k_i.
A reciprocal-lattice point lying on the sphere satisfies the diffraction condition.
The vector from the origin to that reciprocal point is the reciprocal-lattice vector G.
O
kᵢ
G_hkl
Ewald sphere
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 11

## Slide 12
Ewald Geometry → Bragg’s Law
The incident and diffracted wavevectors have the same magnitude.
The angle between k_i and k_f is 2θ.
The reciprocal vector G_hkl closes the triangle: G = k_f − k_i.
Using the triangle geometry gives the Bragg condition.
|G| = 2|k| sinθ
|G| = 1/d
⇒ 1/d = 2 sinθ / λ
⇒ 2d sinθ = λ (n = 1)
Key idea
Bragg diffraction and the Ewald construction are two equivalent descriptions of the same diffraction condition.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 12

## Slide 13
Experimental Method I — Laue Method
Principle
A fixed single crystal is illuminated with polychromatic (white) X-rays.
Different wavelengths satisfy Bragg’s law for different planes.
Arrangement
White X-ray beam → stationary single crystal → photographic film/detector.
Uses
Crystal orientation
Symmetry determination
Detection of crystal imperfections
White X-rays
Crystal
Film
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 13

## Slide 14
Experimental Method II — Rotating Crystal Method
A single crystal is mounted on a rotation axis and exposed to monochromatic X-rays.
As the crystal rotates, different sets of planes enter Bragg condition.
Reflections are recorded on a cylindrical film or detector.
Useful for determining unit-cell dimensions and crystal orientation.
Crystal
Monochromatic X-rays
Cylindrical film / detector
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 14

## Slide 15
Experimental Method III — Powder Photograph Method
Sample
Finely powdered/polycrystalline sample contains crystallites in random orientations.
Beam
Monochromatic X-rays strike the powder. Some crystallites always satisfy Bragg’s law.
Pattern
Diffracted rays form cones; a film/detector records rings or peaks at 2θ.
X-ray beam
Powder
Debye–Scherrer rings
Advantages: rapid phase identification, lattice parameter determination, suitable for polycrystalline materials.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 15

## Slide 16
Comparison of X-Ray Diffraction Methods
Method | Crystal / sample | X-ray | Typical information
Laue | Fixed single crystal | Polychromatic | Orientation, symmetry, defects
Rotating crystal | Single crystal | Monochromatic | Unit-cell dimensions, reflections
Powder photograph | Powder / polycrystal | Monochromatic | Phase ID, d-spacings, lattice parameter
Exam tip
Remember: Laue → white radiation; rotating crystal → single crystal + monochromatic radiation; powder → many random crystallites.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 16

## Slide 17
Powder Method: From Peak Position to d-Spacing
An XRD pattern is plotted as intensity versus 2θ.
For each peak, determine θ = (2θ)/2.
Use Bragg’s law to calculate d_hkl.
For cubic crystals, compare 1/d² with h²+k²+l² to index the peaks.
2θ
Intensity
Peak 1
Peak 2
Peak 3
Peak 4
d = nλ / (2 sinθ)
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 17

## Slide 18
Analysis of a Cubic Crystal by Powder Method
Step 1: Measure the diffraction peak positions 2θ.
Step 2: Calculate θ and sin²θ for each peak.
Step 3: Since d_hkl = a/√(h²+k²+l²), then sin²θ ∝ (h²+k²+l²).
Step 4: Find integer ratios of sin²θ and assign (hkl).
Step 5: Calculate the lattice constant a from each indexed peak and take the consistent value.
sin²θ = (λ² / 4a²)(h²+k²+l²)
a = λ√(h²+k²+l²) / (2 sinθ)
Indexing principle
Compare measured sin²θ ratios with integer sequences of H = h²+k²+l².
For SC: 1, 2, 3, 4, 5, 6, 8…
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 18

## Slide 19
Cubic Crystal: Reflection Selection Rules
Simple Cubic (SC)
All (hkl) are, in principle, allowed.
H = h²+k²+l² sequence begins:
1, 2, 3, 4, 5, 6, 8, 9…
BCC
Reflection allowed when h+k+l is even.
First H values:
2, 4, 6, 8, 10, 12…
FCC
h, k, l are all odd or all even.
First H values:
3, 4, 8, 11, 12, 16…
I ∝ |F_hkl|² × multiplicity × other factors
Systematic absences help identify the Bravais lattice.
Actual intensity also depends on the atomic form factor, multiplicity, temperature and structure factor.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 19

## Slide 20
Worked Example: Cubic Powder Analysis
Given
Cu Kα radiation: λ = 1.5406 Å
Observed peak: 2θ = 44.7°
Assume first order: n = 1
θ = 22.35°
d = λ / (2 sinθ) ≈ 2.03 Å
Indexing example
If the peak is assigned to (111),
H = 3.
a = d√3 ≈ 3.51 Å
Important
One peak alone is not sufficient for reliable identification. Use several indexed peaks and check that the calculated lattice parameter remains consistent.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 20

## Slide 21
Powder Analysis Workflow
1
Record 2θ
Peak positions
2
Calculate θ
θ = 2θ/2
3
Calculate d
Bragg law
4
Calculate sin²θ
Compare ratios
5
Index (hkl)
Use H sequence
6
Calculate a
Check consistency
7
Identify lattice
SC / BCC / FCC
Best practice: average a from several well-indexed reflections.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 21

## Slide 22
What Can X-Ray Diffraction Tell Us?
Crystal Structure
Identify phases and determine crystal system / Bravais lattice.
Lattice Parameter
Calculate a, b, c from peak positions.
Strain & Stress
Peak shifts/broadening can indicate lattice strain.
Crystallite Size
Peak broadening can be analysed using Scherrer relation.
Phase Identification
Compare measured pattern with reference diffraction patterns.
Orientation
Single-crystal methods reveal orientation and symmetry.
D ≈ Kλ / (β cosθ) (Scherrer, for size broadening)
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 22

## Slide 23
Formula Sheet — Must Remember
Reciprocal vector
G_hkl = h a* + k b* + l c*
Plane spacing (cubic)
d_hkl = a / √(h²+k²+l²)
Bragg law
2d sinθ = nλ
Reciprocal magnitude
|G_hkl| = 1/d_hkl (or 2π/d with 2π convention)
Cubic powder relation
sin²θ = (λ²/4a²)(h²+k²+l²)
Lattice parameter
a = λ√H / (2 sinθ), H=h²+k²+l²
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 23

## Slide 24
Common Examination Mistakes
Do not confuse θ (Bragg angle) with 2θ (the angle usually plotted/measured in an XRD pattern).
Do not use d = λ/(sinθ); the correct first-order relation is d = λ/(2sinθ).
Remember that reciprocal-lattice vectors are normal to the corresponding real-space planes.
Do not mix reciprocal-lattice conventions with and without 2π factors.
For cubic indexing, check several peaks and the selection rules—not just one peak.
State clearly whether the radiation is monochromatic or polychromatic in each experimental method.
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 24

## Slide 25
Quick Concept Check
1. What does a reciprocal-lattice point (hkl) represent?
2. Why are X-rays suitable for studying crystal structures?
3. What is the Ewald-sphere criterion for diffraction?
4. Which method uses polychromatic X-rays?
5. In powder diffraction, why do rings appear?
6. For a cubic crystal, how is d_hkl related to a?
7. What is the BCC reflection condition?
8. Why should several peaks be used to determine the lattice parameter?
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 25

## Slide 26
Unit Summary
Reciprocal lattice converts crystal-plane geometry into a lattice of points in reciprocal space.
X-ray diffraction arises from constructive interference of waves scattered by periodic crystal planes.
Bragg’s law: 2d sinθ = nλ.
Ewald construction gives the reciprocal-space condition for diffraction.
Laue, rotating-crystal and powder methods are suited to different experimental situations.
Powder analysis of cubic crystals uses Bragg’s law, sin²θ ratios, indexing and consistency of the lattice parameter.
Diffraction pattern → d-spacing → (hkl) → lattice parameter → crystal structure
B.Sc. II Physics • Crystal Diffraction & Reciprocal Lattice • Dr. Sandip S. Patil 26

## Slide 27
THANK YOU
Questions & Discussion
Reciprocal Lattice • X-Ray Diffraction • Powder Analysis
Dr. Sandip S. Patil • Department of Physics